## Slide 1
IllumiNITE V2 TS Data Review

## Slide 2: Objective
2
Review data collected from testing that was performed by TS (TSC #95835)
Compare performance data between IllumiNITE V2, DPF 2400, and DPF 2400XLP
IllumiNITE V2 tested batches:
  S12180110 (LC - low coat weight ~31 gsm)
  T01230106 (HC – high coat weight ~35gsm)

## Slide 3
3
Chart: Peel Adhesion on Mirror (Standard) Stainless Steel
| Instant | 15min | 24hr | 1wk
IllumiNITE V2 | 2.858 | 3.4313 | 4.5477 | 7.142
2400XLP | 3.301 | 4.0523 | 5.278 | 7.971
2400 | 3.459 | 4.2707 | 5.176 | 7.369
Avery V4000 | 2.546 | 3.155 | 3.038
Mirrored | Product | Instant | 15min | 24hr | 1wk
 | IllumiNITE V2 | 2.86 | 3.43 | 4.55 | 7.14
 | 2400XLP | 3.30 | 4.05 | 5.28 | 7.97
 | 2400 | 3.46 | 4.27 | 5.18 | 7.37
 | Avery V4000 |  | 2.55 | 3.16 | 3.04
Notes: Tested on T0128099 batch

## Slide 4
4
Matte | Product | Instant | 15min | 24hr | 1wk
 | IllumiNITE V2 | 2.46 | 2.96 | 4.72 | 7.11
 | 2400XLP | 3.44 | 4.07 | 5.05 | 6.91
 | 2400 | 3.73 | 3.97 | 5.53 | 7.22
Chart: Peel Adhesion on Matte Stainless Steel
| Instant | 15min | 24hr | 1wk
IllumiNITE V2 | 2.458 | 2.959 | 4.718 | 7.1107
DPF 2400XLP | 3.4387 | 4.0703 | 5.048 | 6.9087
DPF 2400 | 3.728 | 3.9677 | 5.525 | 7.222
Notes: Tested on T0128099 batch

## Slide 5
5
Brushed | Product | Instant | 15min | 24hr | 1wk
 | IllumiNITE V2 | 2.55 | 2.56 | 4.28 | 6.34
 | 2400XLP | 1.84 | 3.50 | 4.67 | 6.83
 | 2400 | 2.59 | 4.00 | 4.63 | 6.62
Chart: Peel Adhesion on Brushed Stainless Steel
| Instant | 15min | 24hr | 1wk
IllumiNITE V2 | 2.5453 | 2.5563 | 4.2777 | 6.3387
DPF 2400XLP | 1.8367 | 3.495 | 4.666 | 6.8283
DPF 2400 | 2.588 | 3.9995 | 4.6283 | 6.619
Notes: Tested on T0128099 batch

## Slide 6: Liner Release
6
Time study of liner release is planned with for next production run
Followed ATM #12 test method
Online coated average taken from QA Test Data
Large discrepancy between TS data vs Online Coat
These batches were 3 and 2 months old (tested on March 25)
Online Coated | 
AVERAGE | 32.9
IllumiNITE V2 Liner Release |  | 
Trial | S12180110(LC) | T01230106(HC)
1 | 74.9 | 98.6
2 | 73.0 | 99.9
3 | 73.0 | 100.4
4 | 85.5 | 101.7
5 | 83.6 | 99.9
Average | 78.0 | 100.1
STDev | 5.4 | 1.0
Avery V4000 | 
AVERAGE | 64.9
Notes: One batch was aged tested and recorded 54 g/2in

## Slide 7: Cut and Weed Data
7
Printed on Roland XR-640, outgas 24hrs (or more), laminated with 3210
Cut on Graphtec FC8600 with red holder (60° blade)
All cut with the same settings
  Force: 23, Speed: 20, Accel: 1, Tangential Mode: ON
No hand assist
Left to Right
Weed within the hour
V2 LC performed poorly initially, but testing was redone later and performed as shown above
Product | Unprinted |  |  | Grey |  |  | Black |  | 
 | 1" | 2" | 3" | 1" | 2" | 3" | 1" | 2" | 3"
V2 LC (~31 gsm) | 86% | 96% | 100% | 96% | 100% | 100% | 96% | 100% | 100%
V2 HC (35 gsm) | 100% | 100% | 100% | 100% | 100% | 100% | 96% | 100% | 100%
2400XLP | 25% | 43% | 60% | 68% | 75% | 96% | 86% | 86% | 93%
2400 | 82% | 89% | 100% | 96% | 96% | 100% | 93% | 96% | 100%

## Slide 8: Cut Text Transfer
8
Unprinted, with 3210, transferred onto Chrysler hood
Cut with same settings as cut/weed test
Medium tack transfer tape was used
Transferred at room temperature
Product | Unprinted |  | 
 | 1" | 2" | 3"
V2 HC | Pass | Pass | Pass

## Slide 9: IllumiNITE V2 LC Cut/Weed
9

## Slide 10: IllumiNITE V2 HC Cut/Weed
10

## Slide 11: DPF 2400 Cut/Weed
11

## Slide 12: DPF 2400XLP Cut/Weed
12

## Slide 13: Conclusion
13
On various finishes of stainless steel panels, IllumiNITE V2 peel adhesion performs comparably to 2400XLP and 2400
IllumiNITE V2 cuts/weeds better than both 2400XLP and 2400
IllumiNITE V2 can be recommended for cut letters down to 2”
IllumiNITE V2 transfers adequately with medium tack transfer tape onto painted vehicle body

## Slide 14
QUESTIONS?